## Slide 1: Prestressed Concrete
Lecture 4

## Slide 2: Cracking Moment
Cracking Moment: The bending moment at which visible cracks develop in prestressed concrete members is generally referred to as the ‘cracking moment’. - After the transfer of prestress to concrete, the soffit of the beam will be under compression. -Gradually, these compressive stresses are balanced by the tensile stresses developed due to the transverse loads on the beam, so that the resultant stress at the bottom fiber is zero. A further increase in loading results in the development of tensile stresses at the soffit of the beam. As concrete is weak in tension, microcracks develop as soon as the tensile strain in concrete exceeds about 80 – 100 x 10–6 units4, and if the loads are further increased, visible cracks appear in the tension zone. -It is generally considered that visible cracks appear when the tensile stresses at the soffit are approximately equal to the modulus of rupture of the material.

## Slide 3: Types of Flexural Failure

## Slide 4: Statically Indeterminate Structures
Advantages of Continuous Members
Continuity in prestressed concrete construction has many advantages. In statically indeterminate prestressed concrete structures, the following benefits are noted:
1. The bending moments are more evenly distributed between the center of span and the supports of members.
2. Reduction in the size of members results in lighter structures.
3. The ultimate load carrying capacity is higher than in a statically determinate structure due to the phenomenon of redistribution of moments.
4. Continuity of the members in framed structures leads to increased stability.
5. Continuous girders are formed by segmental construction using precast units connected by prestressed cables.
6. In continuous post-tensioned girders, the curved cables can be suitably positioned to resist the span and support moments.
7. A reduction in the number of anchorages in a continuous prestressed beam in comparison with a series of simply supported beams. Only one pair of post-tensioning anchorages and a single stressing operation can serve several members.
8. In continuous prestressed structures, the deflections are small as compared to simply supported spans.

## Slide 5: Effect of Prestressing Indeterminate Structures
When an indeterminate structure is prestressed, redundant reactions will develop due to the restraint at the supports.

## Slide 6: Disadvantages
The disadvantages encountered in continuous prestressed concrete members are as follows:
1. Loss of prestress due to friction is noticeable in long cables with reversed curves and considerable curvature.
2. Secondary stresses due to prestressing, creep, shrinkage, and temperature, and settlements of supports may induce very high stresses unless they are controlled or provided for in the design.
3. Cables positioned to cater for secondary moments are not generally suitable to provide the required ultimate moment under a given system of loads.
4. The computation of collapse or ultimate load is influenced by the degree of redistribution of moments in the continuous structure.

## Slide 7: Methods of Achieving Contiuity

## Slide 8: Contiuous Beam

## Slide 9: Methods of Analysis of Secondary Moments
The most used methods are based on the principles of, (a) Three moment theorems (b) Consistent deformation (c) Tendon reaction

## Slide 10: Example: Cracking Moment
A rectangular concrete beam of cross-section 120 mm wide and 300 mm deep is prestressed by a straight cable carrying an effective force of 180 kN at an eccentricity of 50 mm. The beam supports an imposed load of 3.14 kN/m over a span of 6 m. If the modulus of rupture of concrete is 5 N/mm2, evaluate the load factor against cracking assuming the self-weight of concrete as 24 kN/m3.

## Slide 11
P = 180 kN I = 27 x107 mm4 e = 50 mm Z = 18 x 105 mm3 A = 36 xmm2 g = (0.12 x 0.3 x 24) = 0.86 kN/m Total load w = (g + q) = (0.86 + 3.14) = 4 kN/m Stresses due to prestress: (P/A) = (180x106 /36x105 ) = 5 N/mm2 (Pe/Z) =(180x106x50/18x105) = 5 N/mm2 Stresses due to loads: Maximum working moment = (0.125 x 4 x 62) = 18 kN m M/Z = 18x106 /18x10 5 = 10 N/mm2 Stress at the bottom fiber at working load = (5 + 5 – 10) = 0 N/mm2 Stress that can start cracking at the bottom fiber = (mod. of rupture)= 5 N/mm2 Extra moment required to create this stress = (5 x 18 x 105) = (9x 106) N mm = 9 kN m Cracking moment = (18 + 9) = 27 kN m Load factor against cracking = (Cracking moment /Working moment) = (27/18) = 1.5
Solution

## Slide 12: Example: Continuous Beams
A continuous prestressed concrete beam ABC (AB = BC = 10 m) has a uniform rectangular cross-section with a width of 100 mm and depth of 300 mm. The cable carrying an effective prestressing force of 360 kN is parallel to the axis of the beam and located at 100 mm from the soffit. (a) Determine the secondary and resultant moment at the central support B. (b) If the beam supports an imposed load of 1.5 kN/m, calculate the resultant stresses at top and bottom of the beam at B. Assume density of concrete as 24 kN/m3. (c) Locate the resultant line of thrust through beam AB.

## Slide 13: Solution:
Applying the three-moment theorem to the continuous beam ABC shown in Fig. 15.6, (MAB + 2MBA + 2kMBC + kMCB) = (KBA + kKBC) Since the ends A and C are simply supported, MAB = MCB = 0 Also, k = 1 and, MBA = MBC = MB KBA = KBC = ( - 6P/L2 Íexdx) = ( - 6x360/10x10)( - 0.05x10x5) = 54 kNm 4MB = (2 x 54) = 108 kN m SM at B is MB = 27 kN m Resultant moment at B due to prestress = (PM + SM) = [(–360 x 0.05) + 27)] = 9 kN m wd = (1.50 + 0.72) = 2.22 kN m Moment at B due to loads = – (WgL2/8) = - (2.22x102/8) = 27.75 kN m Total resultant moment at B = (9 – 27.75) = –18.75 kN m Stresses at the central support section B are, Top fiber stress = (360x102/100x300) – (18.75x106/1.5x104) = – 0.5 N/mm2 (tension) Bottom fiber stress = (360x106/100x300) + (18.75x106/1.5x104) = +24.5 N/mm2 (compression) Pressure line position At A = –5 cm At B = M/P = ( -18.75x106/360) = –52 mm Resultant moment at center of span = (- Pe/4 + WgL2/16) = ( - 360x0.05/4 + 2.2x102/16) = +9.25 kN m Shift of pressure line from the centroidal axis at mid-span points = ( + 9.25x1000/360) = +26 mm The pressure line location is shown in Fig. 15.6.

## Slide 14: Cont.

## Slide 15: Example
A prestressed beam having a rectangular cross-section with a width of 120 mm and a depth of 300 mm is continuous over two spans, AB = BC = 8 m. The cable with zero eccentricity at the ends and an eccentricity of 50 mm towards the top fibers of the beam over the central support, carries an effective force of 500 kN. (a) Calculate the secondary moment developed at B. (b) If the beam supports concentrated loads of 20 kN each at mid-points of span, evaluate the resultant stresses at the central support section B. (c) Also locate the position of the pressure line at section.

## Slide 16: Solution:
P = 500 kN Zt = Zb = 18 x 105 mm3 Q = 20e = 50 mm A = 36 x 103 mm2 g = 0.86 kN/m, and,L = 8 m MA = MC = 0 KAB = KBC = (- 6P/L2 Í exdx) = -6P/L2(1/2xLxex2/3xL) = - 2Pe Applying the three-moment equation for spans AB and BC, 4MB = (–2Pe – 2Pe) = –4Pe SM at B = MB = –Pe RM at B = (PM – SM) = (+ Pe – Pe) = 0 Moment at B due to self-weight and imposed loads is given by, MB = (- gL2/8 – 3QL/16) = ( - 0.86x 82)/8 – (3x 20x 8)/16 = –36.88 kN m Stresses at section B: At top = (500 X103/36x103) - ( 36.88X 106/18x105) = –6.6 N/mm2 (tension) At bottom = (500 x103/35x103 ) + ( 36.88 x106/18x105) = +34.4 N/mm2 (compression) Position of pressure line from the centroidal axis At B = (MB/P) = (36.88x1000/500) = –73.5 mm (below centroidal axis)